## Slide 1: Chapter 12: Structures & Properties of Ceramics
Ceramics is from Greek keramikos, from keramos ‘pottery’.
Compounds between metallic and non-metallic elements with ionic or covalent inter-atomic bonds.
Metals, ceramics, and polymers are the most important engineering materials.
Ceramics: Resistant to extreme high temperatures and harsh environments.
Applications

## Slide 2: Atomic Bonding in Ceramics
• Bonding:
-- Can be ionic and/or covalent in character.
-- % ionic character increases with difference in
electronegativity of atoms.
Adapted from Fig. 2.7, Callister & Rethwisch 8e. (Fig. 2.7 is adapted from Linus Pauling, The Nature of the Chemical Bond, 3rd edition, Copyright 1939 and 1940, 3rd edition. Copyright 1960 by
Cornell University.)
• Degree of ionic character may be large or small:
SiC: small
CaF2: large

## Slide 3: % Ionic Character
Ionic-Covalent Mixed Bonding
% ionic character =
where XA & XB are Pauling electronegativities.
%)
100
(
x
CaF2: 89%
Al2O3: 63%
SiO2: 51%
Si3N4: 30%
SiC: 12%

## Slide 4: Ceramic Crystal Structures
Oxide structures:
1. Anions are larger than cations. 2. Close packed oxygen in a lattice (usually FCC). 3. Cations fit into interstitial sites among anions. (Octahedral)

## Slide 5: Factors that Determine Crystal Structure
1. Relative sizes of ions – Formation of stable structures:
--maximize the # of oppositely charged ion neighbors.
Adapted from Fig. 12.1, Callister & Rethwisch 8e.
-
-
-
-
+
unstable
-
-
-
-
+
stable
-
-
-
-
+
stable
2. Maintenance of
Charge Neutrality :
--Net charge in ceramic
should be zero.
--Reflected in chemical
formula:
CaF
2
:
Ca
2+
cation
F
-
F
-
anions
+
A
m
X
p
m, p values to achieve charge neutrality

## Slide 7: Coordination # and Ionic Radii
• Coordination # increases with
Adapted from Table 12.2, Callister & Rethwisch 8e.
2
r
cation
r
anion
Coord
#
< 0.155
0.155 - 0.225
0.225 - 0.414
0.414 - 0.732
0.732 - 1.0
3
4
6
8
linear
triangular
tetrahedral
octahedral
cubic
Adapted from Fig. 12.2, Callister & Rethwisch 8e.
Adapted from Fig. 12.3, Callister & Rethwisch 8e.
Adapted from Fig. 12.4, Callister & Rethwisch 8e.
ZnS
(zinc blende)
NaCl
(sodium
chloride)
CsCl
(cesium
chloride)
r
cation
r
anion
To form a stable structure, how many anions can
surround around a cation?

## Slide 8
The most common coordination numbers for ceramic materials are 2, 4, and 6.

## Slide 9: Computation of Minimum Cation-Anion Radius Ratio
Determine minimum rcation/ranion for an octahedral site (C.N. = 6)
a = 2ranion

## Slide 10: Bond Hybridization
Bond Hybridization is possible when there is significant covalent bonding
  hybrid electron orbitals form
  For example for SiC
    XSi = 1.8 and XC = 2.5
    ~ 89% covalent bonding
    Both Si and C prefer sp3 hybridization
    Therefore, for SiC, Si atoms occupy
    tetrahedral sites

## Slide 11: Example Problem: Predicting the Crystal Structure of FeO
• On the basis of ionic radii, what crystal structure
would you predict for FeO?
• Answer:
based on this ratio,
-- coord # = 6 because
0.414 < 0.550 < 0.732
-- crystal structure is NaCl
Data from Table 12.3, Callister & Rethwisch 8e.
Ionic radius (nm)
0.053
0.077
0.069
0.100
0.140
0.181
0.133
Cation
Anion
Al
3+
Fe
2
+
Fe
3+
Ca
2+
O
2-
Cl
-
F
-

## Slide 12: Rock Salt Structure
Same concepts can be applied to ionic solids in general.
Example: NaCl (rock salt) structure
rNa = 0.102 nm
rNa/rCl = 0.564
cations (Na+) prefer octahedral sites
rCl = 0.181 nm
Compute the theoretical density for NaCl.

## Slide 13: MgO and FeO
O2- rO = 0.140 nm
Mg2+ rMg = 0.072 nm
rMg/rO = 0.514
cations prefer octahedral sites
So each Mg2+ (or Fe2+) has 6 neighbor oxygen atoms
Adapted from Fig. 12.2, Callister & Rethwisch 8e.
MgO and FeO also have the NaCl structure

## Slide 14: AX Crystal Structures
Adapted from Fig. 12.3, Callister & Rethwisch 8e.
Cesium Chloride structure:
 Since 0.732 < 0.939 < 1.0, cubic sites preferred
So each Cs+ has 8 neighbor Cl-
AX–Type Crystal Structures include NaCl, CsCl, and zinc blende

## Slide 15: AX2 Crystal Structures
Calcium Fluorite (CaF2)
Cations in cube center positions.
UO2, ThO2, ZrO2, CeO2
Antifluorite structure –
positions of cations and anions reversed
Adapted from Fig. 12.5, Callister & Rethwisch 8e.
Fluorite structure
Only ½ of the cube center positions are occupied by Ca2+ ions.

## Slide 16: ABX3 Crystal Structures
Perovskite structure
Ex: complex oxide
BaTiO3
P. Calculate the Density of BaTiO3

## Slide 17: Silicate Ceramics
Most common elements on earth are Si & O
SiO2 (silica) polymorphic forms are quartz, crystobalite, & tridymite
The strong Si-O bonds lead to a high melting temperature (1710ºC) for this material
Si4+
O2-
Adapted from Figs. 12.9-10, Callister & Rethwisch 8e
crystobalite

## Slide 18: Glass Structure
• Quartz is crystalline
SiO2:
• Basic Unit:
Glass is noncrystalline (amorphous)
• Fused silica is SiO2 to which no impurities have been added
• Other common glasses contain impurity ions such as Na+, Ca2+, Al3+, and B3+
(soda glass)
Adapted from Fig. 12.11, Callister & Rethwisch 8e.
Si0
4
tetrahedron
4-
Si
4+
O
2
-
Si
4+
Na
+
O
2
-

## Slide 19: Layered Silicates
Layered silicates (e.g., clays, mica, talc)
  SiO4 tetrahedra connected together to form 2-D plane
A net negative charge is associated with each (Si2O5)2- unit
Negative charge balanced by adjacent plane rich in positively charged cations
Adapted from Fig. 12.13, Callister & Rethwisch 8e.

## Slide 20: Polymorphic Forms of Carbon
Diamond
  tetrahedral bonding of carbon
    hardest material known
    very high thermal conductivity
  large single crystals – gem stones
  small crystals – used to grind/cut other materials
  diamond thin films
    hard surface coatings – used for cutting tools, medical devices, etc.

## Slide 21
12.15 Compute the theoretical density of diamond given that the C—C distance and bond angle are 0.154 nm and 109.5°, respectively.
How does this value compare with the measured density (3.51 g/cm3)?

## Slide 22: Polymorphic Forms of Carbon (cont)
Graphite
  layered structure – parallel hexagonal arrays of carbon atoms
  weak van der Waal’s forces between layers
  planes slide easily over one another -- good lubricant
Adapted from Fig. 12.17, Callister & Rethwisch 8e.

## Slide 23: Polymorphic Forms of Carbon (cont) Fullerenes and Nanotubes
Fullerenes – spherical cluster of 60 carbon atoms, C60
  Like a soccer ball
Carbon nanotubes – sheet of graphite rolled into a tube
  Ends capped with fullerene hemispheres
Adapted from Figs. 12.18 & 12.19, Callister & Rethwisch 8e.