## Slide 1: Chap 20: Magnetic Properties
Why study magnetic properties?
Magnetic materials are in the heart of many current technological systems.
Electric generators
Transformers Hard Disk in a computer Speakers
Microphones
Electric motors

## Slide 2: Generation of a Magnetic Field -- Vacuum
• Created by current through a coil:
I = current (ampere)
N = total number of turns
 = length of each turn (m)

## Slide 3: Generation of a Magnetic Field -- within a Solid Material
• A magnetic field is induced in the material
current I
B = Magnetic field (tesla) inside the material
• Relative permeability (dimensionless)
B
χm = Magnetic Susceptibility. Measure of a material’s magnetic response.
mBvac

## Slide 4
Types of Magnetism

## Slide 5: Magnetic Responses for 4 Types
Adapted from Fig. 20.5(a), Callister & Rethwisch 8e.
No Applied
Magnetic Field
Applied
Magnetic Field
(1) diamagnetic
none
opposing
Adapted from Fig. 20.5(b), Callister & Rethwisch 8e.
(2) paramagnetic
random
aligned
Adapted from Fig. 20.7, Callister & Rethwisch 8e.
(3) ferromagnetic
(4) ferrimagnetic
aligned
aligned

## Slide 6
Un paired electrons are necessary for magnetic materials

## Slide 7: Origins of Magnetic Moments
• Magnetic moments arise from electron motions and the spins on electrons.
• Net atomic magnetic moment:
-- sum of moments from all electrons.
Adapted from Fig. 20.4, Callister & Rethwisch 8e.
magnetic moments
electron
nucleus
electron
spin
electron orbital motion
electron spin

## Slide 8
The most fundamental magnetic moment
Bohr Magneton

## Slide 9: Ferromagnetism
Certain metallic materials possess a permanent magnetic moment in the absence of
an external field and manifest very large and permanent magnetizations. These are
the characteristics of ferromagnetism, and they are displayed by the transition metals
iron (as BCC α-ferrite), cobalt, nickel, and some rare earth metals such as gadolinium
(Gd). Magnetic susceptibilities as high as 106 are possible for ferromagnetic materials.
B = µ0 M
B = Bvac + 0M
This mutual spin alignment exists over relatively large-volume regions of the crystal called domains. The maximum possible magnetization, or saturation magnetization, of a ferromagnetic
material represents the magnetization (M) that results when all the magnetic dipoles in a solid piece are mutually aligned with the external field; there is also a corresponding saturation flux density (B).
For each of iron, cobalt, and nickel, the net magnetic moments per atom are 2.22, 1.72, and 0.60 Bohr magnetons, respectively.
Bohr magneton = 9.27 x 10-24 A.m2

## Slide 10: Iron: 2.2 Bohr Magnetons
Confirm that there are 2.2 Bohr magnetons associated with each iron atom, given that the saturation magnetization is 1.70  106 A/m, that iron has a BCC crystal structure, and that the unit cell edge length is 0.2866 nm.

## Slide 11: Problem 20.7
Compute (a) the saturation magnetization and (b) the saturation magnetic field for iron, which has a net magnetic moment per atom of 2.2 Bohr magnetons and a density of 7.87 g/cm3. Bohr magneton = 9.27 x 10-24 A.m2.

## Slide 12: Influence of Temperature on Magnetic Behavior
With increasing temperature, the saturation magnetization diminishes gradually and then abruptly drops to zero at Curie Temperature, Tc.

## Slide 13: Magnetic Domains

## Slide 14: Domains in Ferromagnetic & Ferrimagnetic Materials
• As the applied field (B) increases the magnetic domains change shape and size by movement of domain boundaries.
Adapted from Fig. 20.13, Callister & Rethwisch 8e. (Fig. 20.13 adapted from O.H. Wyatt and D. Dew-Hughes, Metals, Ceramics, and Polymers, Cambridge University Press, 1974.)
Applied Magnetic Field (B)
Magnetic
induction (B)
0
B
sat
B= 0
B
B
B
B
B
• “Domains” with
aligned magnetic
moment grow at
expense of poorly
aligned ones!

## Slide 15: Hysteresis and Permanent Magnetization
Adapted from Fig. 20.14, Callister & Rethwisch 8e.
B vac
Stage 1. Initial (unmagnetized state)
B
Stage 4. Coercivity, BC Negative Bvac needed to demagnitize!
• The magnetic hysteresis phenomenon
Stage 2. Apply Bvac, align domains
Stage 3. Remove Bvac, alignment
remains! => permanent magnet!
Stage 5. Apply –B vac, align domains
Stage 6. Close the hysteresis loop

## Slide 16: Magnetic Anisotropy
Easy magnetization direction:
Ni- [111], Fe- [100], Co- [0001].
Hard magnetization direction:
Ni- [100], Fe- [111], Co-

## Slide 17: Hard and Soft Magnets
Electric generators:
Hard permanent magnets
Transformers: Soft permanent magnets
Hard Disk: In between hard and soft.

## Slide 18: Hard and Soft Magnetic Materials
18
Hard magnetic materials:
-- large coercivities
-- used for permanent magnets
-- add particles/voids to
inhibit domain wall motion
-- example: tungsten steel --
Bc = 5900 amp-turn/m)
Soft magnetic materials:
-- small coercivities
-- used for transformers
-- example: commercial iron 99.95 Fe
Adapted from Fig. 20.19, Callister & Rethwisch 8e. (Fig. 20.19 from K.M. Ralls, T.H. Courtney, and J. Wulff, Introduction to Materials Science and Engineering, John Wiley and Sons, Inc., 1976.)
H
B
Hard
Soft
Notes: 18

## Slide 19: Iron-Silicon Alloy (97 wt% Fe – 3 wt% Si) in Transformer Cores
Transformer cores require soft magnetic materials, which are easily magnetized and de-magnetized, and have high electrical resistivity.
Energy losses in transformers could be minimized if their cores were fabricated such that the easy magnetization direction is parallel to the direction of the applied magnetic field.

## Slide 20: Magnetic Storage
• Digitized data in the form of electrical signals are transferred to and recorded digitally on a magnetic medium (tape or disk)
• This transference is accomplished by a recording system that consists of a read/write head
Fig. 20.23, Callister & Rethwisch 8e.
-- “write” or record data by applying a magnetic field that aligns domains in small regions of the recording medium
-- “read” or retrieve data from medium by sensing changes in magnetization
http://www.ehow.com/how-does_4968711_solid-state-hard-drives-work.html

## Slide 21
Magnetic Storage Media Types
Fig. 20.25, Callister & Rethwisch 8e. (Fig. 20.25 from Seagate Recording Media)
80 nm
-- CoCr alloy grains (darker regions) separated by oxide grain boundary segregant layer (lighter regions)
-- Magnetization direction of each grain is perpendicular to plane of disk
• Hard disk drives (granular/perpendicular media):
• Recording tape (particulate media):
Fig. 20.24, Callister & Rethwisch 8e. (Fig. 20.24 courtesy Fuji Film Inc., Recording Media Division)
~ 500 nm
-- Acicular (needle-shaped) ferromagnetic metal alloy particles
-- Tabular (plate-shaped) ferrimagnetic barium-ferrite particles
~ 500 nm

## Slide 22: Superconductivity
TC = critical temperature
= temperature below which material is superconductive
Copper (normal)
Mercury
4.2 K
Fig. 20.26, Callister & Rethwisch 8e.
Found in 26 metals and hundreds of alloys & compounds

## Slide 23: Critical Properties of Superconductive Materials
TC = critical temperature - if T > TC not superconducting JC = critical current density - if J > JC not superconducting BC = critical magnetic field - if B > BC not superconducting
Fig. 20.27, Callister & Rethwisch 8e.

## Slide 24: Meissner Effect
Superconductors expel magnetic fields
This is why a superconductor will float above a magnet
normal
superconductor
Fig. 20.28, Callister & Rethwisch 8e.

## Slide 25: Advances in Superconductivity
Research in superconductive materials was stagnant for many years.
  Everyone assumed TC,max was about 23 K
  Many theories said it was impossible to increase TC beyond this value
1987- new materials were discovered with TC > 30 K
  ceramics of form Ba1-x Kx BiO3-y
  Started enormous race
    Y Ba2Cu3O7-x TC = 90 K
    Tl2Ba2Ca2Cu3Ox TC = 122 K
    difficult to make since oxidation state is very important
The major problem is that these ceramic materials are inherently brittle.
Notes: Suddenly everyone was doing superconductivity. Everyone was doing similar work, making discoveries, & rushing to publish so they could claim to have done it first. Practically, daily new high temp. records were set.

## Slide 26: Summary
• A magnetic field is produced when a current flows through a wire coil.
• Magnetic induction (B):
-- an internal magnetic field is induced in a material that is situated within an external magnetic field
-- magnetic moments result from electron interactions with the applied magnetic field
• Types of material responses to magnetic fields are:
-- ferrimagnetic and ferromagnetic (large magnetic susceptibilities)
-- paramagnetic (small and positive magnetic susceptibilities)
-- diamagnetic (small and negative magnetic susceptibilities)
• Types of ferrimagnetic and ferromagnetic materials:
-- Hard: large coercivities
-- Soft: small coercivities
• Magnetic storage media:
-- particulate barium-ferrite in polymeric film (tape)
-- thin film Co-Cr alloy (hard drive)