## Slide 1: Chap 20: Magnetic Properties
a) Transmission electron micrograph showing the microstructure of the perpendicular magnetic recording medium used in hard-disk drives.
b) Magnetic storage hard disks used in laptop (left) and desktop (right) computers. c) Inside of a hard disk drive.
d) Laptop computer

## Slide 2: Chapter 20: Magnetic Properties
ISSUES TO ADDRESS...
• What are the important magnetic properties?
• How do we explain magnetic phenomena?
• How does magnetic memory storage work?
• How are magnetic materials classified?
• What is superconductivity and how do magnetic fields effect the behavior of superconductors?

## Slide 3: Generation of a Magnetic Field -- Vacuum
• Created by current through a coil:
I = current (ampere)
I
B
N = total number of turns
 = length of each turn (m)
B = magnetic field (tesla)

## Slide 4: Generation of a Magnetic Field -- Vacuum
• Created by current through a coil:
• Computation of the applied magnetic field, H:
I = current (ampere)
H
I
B0
N = total number of turns
B0 = 0H
permeability of a vacuum (1.257 x 10-6 Henry/m)
• Computation of the magnetic flux density in a vacuum, B0:
 = length of each turn (m)
H = applied magnetic field (ampere-turns/m)
B0 = magnetic flux density in a vacuum (tesla)

## Slide 5: Generation of a Magnetic Field -- within a Solid Material
• A magnetic field is induced in the material
current I
B = Magnetic Induction (tesla) inside the material
applied
magnetic field H
B = H
permeability of a solid
• Relative permeability (dimensionless)
B

## Slide 6: Generation of a Magnetic Field -- within a Solid Material (cont.)
cm is a measure of a material’s magnetic response relative to a vacuum
Magnetic susceptibility (dimensionless)
• Magnetization
M = mH
B = 0H + 0 mH
• Combining the above two equations:
• B in terms of H and M
B = 0H + 0M
H
B
vacuum cm = 0
cm
cm
> 0
< 0
permeability of a vacuum:
(1.26 x 10-6 Henry/m)
= (1 + m)0H

## Slide 7
20.1 A coil of wire 0.20 m long and having 200 turns carries a current of 10 A.
(a) What is the magnitude of the magnetic field strength H?
(b) Compute the flux density B if the coil is in a vacuum.
(c) Compute the flux density inside a bar of titanium that is positioned within the coil. The susceptibility for titanium is found in Table 20.2.
(d) Compute the magnitude of the magnetization M.

## Slide 8: Origins of Magnetic Moments
• Magnetic moments arise from electron motions and the spins on electrons.
• Net atomic magnetic moment:
-- sum of moments from all electrons.
• Four types of response...
Adapted from Fig. 20.4, Callister & Rethwisch 8e.
magnetic moments
electron
nucleus
electron
spin
electron orbital motion
electron spin

## Slide 9: Types of Magnetism
Plot adapted from Fig. 20.6, Callister & Rethwisch 8e. Values and materials from Table 20.2 and discussion in Section 20.4, Callister & Rethwisch 8e.
B (tesla)
H (ampere-turns/m)
vacuum
(
cm
= 0)
(1) diamagnetic (
cm
~ -10-5)
e.g., Al2O3, Cu, Au, Si, Ag, Zn
(3) ferromagnetic e.g. Fe3O4, NiFe2O4
(4) ferrimagnetic e.g. ferrite(), Co, Ni, Gd
(
cm
as large as
106
!)
(2) paramagnetic (
e.g., Al, Cr, Mo, Na, Ti, Zr
cm
~ 10-4)

## Slide 10: Magnetic Responses for 4 Types
Adapted from Fig. 20.5(a), Callister & Rethwisch 8e.
No Applied
Magnetic Field (H = 0)
Applied
Magnetic Field (H)
(1) diamagnetic
none
opposing
Adapted from Fig. 20.5(b), Callister & Rethwisch 8e.
(2) paramagnetic
random
aligned
Adapted from Fig. 20.7, Callister & Rethwisch 8e.
(3) ferromagnetic
(4) ferrimagnetic
aligned
aligned

## Slide 11: Influence of Temperature on Magnetic Behavior
With increasing temperature, the saturation magnetization diminishes gradually and then abruptly drops to zero at Curie Temperature, Tc.

## Slide 12: Magnetic Domains

## Slide 13: Domains in Ferromagnetic & Ferrimagnetic Materials
• As the applied field (H) increases the magnetic domains change shape and size by movement of domain boundaries.
Adapted from Fig. 20.13, Callister & Rethwisch 8e. (Fig. 20.13 adapted from O.H. Wyatt and D. Dew-Hughes, Metals, Ceramics, and Polymers, Cambridge University Press, 1974.)
Applied Magnetic Field (H)
Magnetic
induction (B)
0
B
sat
H = 0
H
H
H
H
H
• “Domains” with
aligned magnetic
moment grow at
expense of poorly
aligned ones!

## Slide 14: Hysteresis and Permanent Magnetization
Adapted from Fig. 20.14, Callister & Rethwisch 8e.
H
Stage 1. Initial (unmagnetized state)
B
Stage 4. Coercivity, HC Negative H needed to demagnitize!
• The magnetic hysteresis phenomenon
Stage 2. Apply H, align domains
Stage 3. Remove H, alignment
remains! => permanent magnet!
Stage 5. Apply -H, align domains
Stage 6. Close the hysteresis loop

## Slide 15: Magnetic Anisotropy
Easy magnetization direction:
Ni- [111], Fe- [100], Co- [0001].
Hard magnetization direction:
Ni- [100], Fe- [111], Co-

## Slide 16: Hard and Soft Magnetic Materials
16
Hard magnetic materials:
-- large coercivities
-- used for permanent magnets
-- add particles/voids to
inhibit domain wall motion
-- example: tungsten steel --
Hc = 5900 amp-turn/m)
Soft magnetic materials:
-- small coercivities
-- used for electric motors
-- example: commercial iron 99.95 Fe
Adapted from Fig. 20.19, Callister & Rethwisch 8e. (Fig. 20.19 from K.M. Ralls, T.H. Courtney, and J. Wulff, Introduction to Materials Science and Engineering, John Wiley and Sons, Inc., 1976.)
H
B
Hard
Soft
Notes: 16

## Slide 17: Iron-Silicon Alloy (97 wt% Fe – 3 wt% Si) in Transformer Cores
Transformer cores require soft magnetic materials, which are easily magnetized and de-magnetized, and have high electrical resistivity.
Energy losses in transformers could be minimized if their cores were fabricated such that the easy magnetization direction is parallel to the direction of the applied magnetic field.

## Slide 18: Magnetic Storage
• Digitized data in the form of electrical signals are transferred to and recorded digitally on a magnetic medium (tape or disk)
• This transference is accomplished by a recording system that consists of a read/write head
Fig. 20.23, Callister & Rethwisch 8e.
-- “write” or record data by applying a magnetic field that aligns domains in small regions of the recording medium
-- “read” or retrieve data from medium by sensing changes in magnetization
http://www.ehow.com/how-does_4968711_solid-state-hard-drives-work.html
https://www.youtube.com/watch?v=f3BNHhfTsvk

## Slide 19
Magnetic Storage Media Types
Fig. 20.25, Callister & Rethwisch 8e. (Fig. 20.25 from Seagate Recording Media)
80 nm
-- CoCr alloy grains (darker regions) separated by oxide grain boundary segregant layer (lighter regions)
-- Magnetization direction of each grain is perpendicular to plane of disk
• Hard disk drives (granular/perpendicular media):
• Recording tape (particulate media):
Fig. 20.24, Callister & Rethwisch 8e. (Fig. 20.24 courtesy Fuji Film Inc., Recording Media Division)
~ 500 nm
-- Acicular (needle-shaped) ferromagnetic metal alloy particles
-- Tabular (plate-shaped) ferrimagnetic barium-ferrite particles
~ 500 nm

## Slide 20: Superconductivity
TC = critical temperature
= temperature below which material is superconductive
Copper (normal)
Mercury
4.2 K
Fig. 20.26, Callister & Rethwisch 8e.
Found in 26 metals and hundreds of alloys & compounds

## Slide 21: Critical Properties of Superconductive Materials
TC = critical temperature - if T > TC not superconducting JC = critical current density - if J > JC not superconducting HC = critical magnetic field - if H > HC not superconducting
Fig. 20.27, Callister & Rethwisch 8e.

## Slide 22: Meissner Effect
Superconductors expel magnetic fields
This is why a superconductor will float above a magnet
normal
superconductor
Fig. 20.28, Callister & Rethwisch 8e.

## Slide 23: Advances in Superconductivity
Research in superconductive materials was stagnant for many years.
  Everyone assumed TC,max was about 23 K
  Many theories said it was impossible to increase TC beyond this value
1987- new materials were discovered with TC > 30 K
  ceramics of form Ba1-x Kx BiO3-y
  Started enormous race
    Y Ba2Cu3O7-x TC = 90 K
    Tl2Ba2Ca2Cu3Ox TC = 122 K
    difficult to make since oxidation state is very important
The major problem is that these ceramic materials are inherently brittle.
Notes: Suddenly everyone was doing superconductivity. Everyone was doing similar work, making discoveries, & rushing to publish so they could claim to have done it first. Practically, daily new high temp. records were set.

## Slide 24: Summary
• A magnetic field is produced when a current flows through a wire coil.
• Magnetic induction (B):
-- an internal magnetic field is induced in a material that is situated within an external magnetic field (H).
-- magnetic moments result from electron interactions with the applied magnetic field
• Types of material responses to magnetic fields are:
-- ferrimagnetic and ferromagnetic (large magnetic susceptibilities)
-- paramagnetic (small and positive magnetic susceptibilities)
-- diamagnetic (small and negative magnetic susceptibilities)
• Types of ferrimagnetic and ferromagnetic materials:
-- Hard: large coercivities
-- Soft: small coercivities
• Magnetic storage media:
-- particulate barium-ferrite in polymeric film (tape)
-- thin film Co-Cr alloy (hard drive)