## Slide 1: Chapter 19: Thermal Properties
ISSUES TO ADDRESS...
• How do materials respond to the application of heat?
• How do we define and measure...
-- heat capacity?
-- thermal expansion?
-- thermal conductivity?
-- thermal shock resistance?
• How do the thermal properties of ceramics, metals, and polymers differ?

## Slide 2: Thermal Conductivity
The ability of a material to transport heat.
temperature
gradient
thermal conductivity (J/m-K-s)
heat flux
(J/m2-s)
• Atomic perspective: Atomic vibrations and free electrons in hotter regions transport energy to cooler regions.
T2
T2 > T1
T1
x1
x2
heat flux
Fourier’s Law

## Slide 3: Thermal Conductivity: Comparison
increasing k
• Polymers
Polypropylene
0.12
Polyethylene
0.46-0.50
Polystyrene
0.13
Teflon
0.25
vibration/rotation of chain molecules
• Ceramics
Magnesia (MgO)
38
Alumina (Al2O3)
39
Soda-lime glass
1.7
Silica (cryst. SiO2)
1.4
atomic vibrations
• Metals
Aluminum
247
Steel
52
Tungsten
178
Gold
315
atomic vibrations and motion of free electrons
k (W/m-K)
Energy Transfer Mechanism
Material
Selected values from Table 19.1, Callister & Rethwisch 8e.

## Slide 4
19.14 (a) Calculate the heat flux through a sheet of steel 10 mm (0.39 in.) thick if the temperatures at the two faces are 300 and 100°C (572 and 212°F); assume steady-state heat flow. (b) What is the heat loss per hour if the area of the sheet is 0.25 m2 (2.7 ft2)? (c) What will be the heat loss per hour if soda–lime glass instead of steel is used? (d) Calculate the heat loss per hour if steel is used and the thickness is increased to 20 mm (0.79 in.).

## Slide 5: Thermal Stresses
• Occur due to:
-- restrained thermal expansion/contraction
-- temperature gradients that lead to differential dimensional changes
Thermal stress

Upon heating, the stress is compressive (σ < 0), because rod expansion has been constrained.
Upon cooling, the stress is tensile (σ > 0).

## Slide 6
Ex-Prob 19.1: A brass rod is stress-free at room temperature (20ºC). It is heated up, but prevented from lengthening. At what temperature does the stress reach -172 MPa? (For brass, assume a modulus of elasticity of 100 GPa and the coef. Linear thermal exp. = 20x10-6 (C0)-1)

## Slide 7: Thermal Shock Resistance
• Occurs due to: nonuniform heating/cooling
• Ex: Assume top thin layer is rapidly cooled from T1 to T2
Tension develops at surface
Critical temperature difference
for fracture (set s = sf)
set equal
• Large TSR when is large
Temperature difference that
can be produced by cooling:
s
rapid quench
resists contraction
tries to contract during cooling
T2
T1
•

## Slide 8: Thermal Protection System
• Application:
Space Shuttle Orbiter
• Silica tiles (400-1260ºC):
-- large scale application
-- microstructure:
Fig. 19.2W, Callister 6e. (Fig. 19.2W adapted from L.J. Korb, C.A. Morant, R.M. Calland, and C.S. Thatcher, "The Shuttle Orbiter Thermal Protection System", Ceramic Bulletin, No. 11, Nov. 1981, p. 1189.)
Fig. 19.3W, Callister 5e. (Fig. 19.3W courtesy the National Aeronautics and Space Administration.)
Fig. 19.4W, Callister 5e. (Fig. 219.4W courtesy Lockheed Aerospace Ceramics
Systems, Sunnyvale, CA.)
reinf C-C
(1650ºC)
Re-entry T
Distribution
silica tiles
(400-1260ºC)
nylon felt, silicon rubber
coating (400ºC)
~90% porosity!
Si fibers
bonded to one
another during
heat treatment.
100 mm
Chapter-opening photograph, Chapter 23, Callister 5e (courtesy of the National Aeronautics and Space Administration.)

## Slide 9: Summary
The thermal properties of materials include:
• Heat capacity:
-- energy required to increase a mole of material by a unit T
-- energy is stored as atomic vibrations
• Coefficient of thermal expansion:
-- the size of a material changes with a change in temperature
-- polymers have the largest values
• Thermal conductivity:
-- the ability of a material to transport heat
-- metals have the largest values
• Thermal shock resistance:
-- the ability of a material to be rapidly cooled and not fracture
-- is proportional to