## Slide 1: Chapter 6: Mechanical Properties
ISSUES TO ADDRESS...
• Stress and strain: What are they and why are
they used instead of load and deformation?
• Elastic behavior: When loads are small, how much
deformation occurs? What materials deform least?
• Plastic behavior: At what point does permanent deformation occur? What materials are most resistant to permanent deformation?
• Toughness and ductility: What are they and how
do we measure them?

## Slide 2: Elastic Deformation
Elastic means reversible!
2. Small load
F
d
bonds
stretch
1. Initial
3. Unload
return to
initial
F
d
Linear-
elastic
Non-Linear-
elastic

## Slide 3: Plastic Deformation (Metals)
Plastic means permanent!
F
d
linear
elastic
linear
elastic
d
plastic
1. Initial
2. Small load
3. Unload
planes
still
sheared
F
d
elastic + plastic
bonds
stretch
& planes
shear
d
plastic
Demo: Hooke’s law experiment

## Slide 4: Engineering Stress
 Stress has units: N/m2 or lbf /in2
• Shear stress, t:
Area, Ao
F
t
F
t
F
s
F
F
F
s
t
=
F
s
A
o
• Tensile stress, s:
original area
before loading
s
=
F
t
A
o
2
f
2
m
N
or
in
lb
=
Area, Ao
F
t
F
t

## Slide 5: Common States of Stress
• Simple tension: cable
o
s
=
F
A
o
t
=
F
s
A
s
s
M
M
A
o
2R
F
s
A
c
• Torsion (a form of shear): drive shaft
Ski lift (photo courtesy P.M. Anderson)
A
o
= cross sectional
area (when unloaded)
F
F

## Slide 6: OTHER COMMON STRESS STATES (i)
(photo courtesy P.M. Anderson)
Canyon Bridge, Los Alamos, NM
o
s
=
F
A
• Simple compression:
Note: compressive
structure member
(s < 0 here).
(photo courtesy P.M. Anderson)
A
o
Balanced Rock, Arches
National Park

## Slide 7: OTHER COMMON STRESS STATES (ii)
• Bi-axial tension:
• Hydrostatic compression:
Pressurized tank
s < 0
h
(photo courtesy
P.M. Anderson)
(photo courtesy
P.M. Anderson)
Fish under water
s
z
> 0
s
q
> 0

## Slide 8: Engineering Strain
• Tensile strain:
• Lateral strain:
Strain is always
dimensionless.
• Shear strain:
q
90º
90º - q
y
x
q
g = Dx/y = tan
e
=
d
L
o
Adapted from Fig. 6.1(a) and (c), Callister & Rethwisch 8e.
d
/2
L
o
w
o
-
d
e
L
=
L
w
o
d
L
/2

## Slide 9: Stress-Strain Testing
• Typical tensile test machine
Adapted from Fig. 6.3, Callister & Rethwisch 8e. (Fig. 6.3 is taken from H.W. Hayden, W.G. Moffatt, and J. Wulff, The Structure and Properties of Materials, Vol. III, Mechanical Behavior, p. 2, John Wiley and Sons, New York, 1965.)
specimen
extensometer
• Typical tensile specimen
Adapted from Fig. 6.2,
Callister & Rethwisch 8e.
gauge
length

## Slide 10: Linear Elastic Properties
• Modulus of Elasticity, E:
(also known as Young's modulus)
• Hooke's Law:
s = E e
s
Linear-
elastic
E
e
F
F
simple
tension
test

## Slide 11: Elastic and Shear Moduli

## Slide 12: Problems
6.3 A specimen of aluminum having a rectangular cross section 10 mm  12.7 mm (0.4 in.  0.5 in.) is pulled in tension with 35,500 N (8000 lbf) force, producing only elastic deformation. Calculate the resulting strain.
6.5 A steel bar 100 mm (4.0 in.) long and having a square cross section 20 mm (0.8 in.) on an edge is pulled in tension with a load of 89,000 N (20,000 lbf), and experiences an elongation of 0.10 mm (4.0  10-3 in.). Assuming that the deformation is entirely elastic, calculate the elastic modulus of the steel.

## Slide 13: Poisson's ratio, n
• Poisson's ratio, n:
   > 0.50 density increases
   < 0.50 density decreases (voids form)
eL
e
-n
e
n
=
-
L
e
metals: n ~ 0.33 ceramics: n ~ 0.25 polymers: n ~ 0.40
https://www.youtube.com/watch?v=IoYQ1ddT2MU

## Slide 14: Mechanical Properties
Slope of stress strain plot (which is proportional to the elastic modulus) depends on bond strength of metal
Adapted from Fig. 6.7,
Callister & Rethwisch 8e.

## Slide 15: Other Elastic Properties
• Elastic Shear
modulus, G:
t
G
g
t = G g
simple
torsion
test
M
M
• Special relations for isotropic materials:
2(1 + n)
E
G
=
3(1 - 2n)
E
K
=
• Elastic Bulk
modulus, K:
pressure
test: Init.
vol =Vo.
Vol chg.
= DV
P
P
P
P = -
K
D
V
V
o
P
D
V
K
V
o

## Slide 16: E = 2G (1+ ν)
6.18 A cylindrical specimen of a hypothetical metal alloy is stressed in compression. If its original and final diameters are 20.000 and 20.025 mm, respectively, and its final length is 74.96 mm, compute its original length if the deformation is totally elastic. The elastic and shear moduli for this alloy are 105 GPa and 39.7 GPa, respectively.

## Slide 17: Young’s Moduli: Comparison
Metals
Alloys
Graphite
Ceramics
Semicond
Polymers
Composites
/fibers
E(GPa)
Based on data in Table B.2,
Callister & Rethwisch 8e.
Composite data based on
reinforced epoxy with 60 vol%
of aligned
carbon (CFRE),
aramid (AFRE), or
glass (GFRE)
fibers.
109 Pa
0.2
8
0.6
1
Magnesium,
Aluminum
Platinum
Silver, Gold
Tantalum
Zinc, Ti
Steel, Ni
Molybdenum
G
raphite
Si crystal
Glass
-
soda
Concrete
Si nitride
Al oxide
PC
Wood( grain)
AFRE( fibers)
*
CFRE
*
GFRE*
Glass fibers only
Carbon
fibers only
A
ramid fibers only
Epoxy only
0.4
0.8
2
4
6
10
2
0
4
0
6
0
8
0
10
0
2
00
6
00
8
00
10
00
1200
4
00
Tin
Cu alloys
Tungsten
<100>
<111>
Si carbide
Diamond
PTF
E
HDP
E
LDPE
PP
Polyester
PS
PET
C
FRE( fibers)
*
G
FRE( fibers)*
G
FRE(|| fibers)*
A
FRE(|| fibers)*
C
FRE(|| fibers)*

## Slide 18: Plastic (Permanent) Deformation
(at lower temperatures, i.e. T < Tmelt/3)
• Simple tension test:
engineering stress, s
engineering strain, e
Elastic+Plastic
at larger stress
ep
plastic strain
Elastic
initially
Adapted from Fig. 6.10(a),
Callister & Rethwisch 8e.
permanent (plastic)
after load is removed

## Slide 19: Yield Strength, sy
• Stress at which noticeable plastic deformation has
occurred.
when ep = 0.002
y = yield strength
Note: for 2 inch sample
 = 0.002 = z/z
 z = 0.004 in
Adapted from Fig. 6.10(a),
Callister & Rethwisch 8e.
tensile stress,
s
engineering strain,
e
sy
ep
= 0.002

## Slide 20: Yield Strength : Comparison
Room temperature values
Based on data in Table B.4,
Callister & Rethwisch 8e.
a = annealed
hr = hot rolled
ag = aged
cd = cold drawn
cw = cold worked
qt = quenched & tempered
Graphite/
Ceramics/
Semicond
Metals/
Alloys
Composites/
fibers
Polymers
Yield strength,
s
y
(MPa)
PVC
Hard to measure
,
since in tension, fracture usually occurs before yield.
Nylon 6,6
LDPE
70
20
40
60
50
100
10
30
200
300
400
500
600
700
1000
2000
Tin (pure)
Al
(6061)
a
Al
(6061)
ag
Cu
(71500)
hr
Ta
(pure)
Ti
(pure)
a
Steel
(1020)
hr
Steel
(1020)
cd
Steel
(4140)
a
Steel
(4140)
qt
Ti
(5Al-2.5Sn)
a
W
(pure)
Mo (pure)
Cu
(71500)
cw
Hard to measure,
in ceramic matrix and epoxy matrix composites, since
in tension, fracture usually occurs before yield.
H
DPE
PP
humid
dry
PC
PET
¨

## Slide 21: Tensile Strength, TS
• Metals: occurs when noticeable necking starts.
• Polymers: occurs when polymer backbone chains are
aligned and about to break.
Adapted from Fig. 6.11, Callister & Rethwisch 8e.
y
strain
Typical response of a metal
F = fracture or
ultimate
strength
Neck – acts as stress concentrator
engineering
TS
stress
engineering strain
• Maximum stress on engineering stress-strain curve.

## Slide 22: Figure 6.12
From the behavior shown below for a brass specimen, Find:
Modulus of elasticity
Yield strength at a strain
offset of 0.002.
3. Max load by a cylindrical
specimen, dia = 12.8 mm.
4. Change in length of a
specimen, 250 mm long,
subjected to a tensile
stress of 345 MPa.

## Slide 23: Tensile Strength: Comparison
Si crystal
<100>
Graphite/
Ceramics/
Semicond
Metals/
Alloys
Composites/
fibers
Polymers
Tensile
strength, TS
(MPa)
PVC
Nylon 6,6
10
100
200
300
1000
Al
(6061)
a
Al
(6061)
ag
Cu
(71500)
hr
Ta
(pure)
Ti
(pure)
a
Steel
(1020)
Steel
(4140)
a
Steel
(4140)
qt
Ti
(5Al-2.5Sn)
a
W
(pure)
Cu
(71500)
cw
L
DPE
PP
PC
PET
20
30
40
2000
3000
5000
Graphite
Al oxide
Concrete
Diamond
Glass-soda
Si nitride
H
DPE
wood
( fiber)
wood(|| fiber)
1
GFRE
(|| fiber)
GFRE
( fiber)
C
FRE
(|| fiber)
C
FRE
( fiber)
A
FRE
(|| fiber)
A
FRE( fiber)
E-glass fib
C
fibers
Aramid
fib
Based on data in Table B.4,
Callister & Rethwisch 8e.
a = annealed
hr = hot rolled
ag = aged
cd = cold drawn
cw = cold worked
qt = quenched & tempered
AFRE, GFRE, & CFRE =
aramid, glass, & carbon
fiber-reinforced epoxy
composites, with 60 vol%
fibers.
Room temperature values

## Slide 24: Ductility
Ductility is another important mechanical property.
It is a measure of the degree of plastic deformation that has been sustained at fracture.
If very little or no plastic deformation  brittle.

## Slide 25: Ductility
• Plastic tensile strain at failure: (percent elongation)
• Another ductility measure: (reduction in area)
100
x
A
A
A
RA
%
o
f
o
-
=
x 100
L
L
L
EL
%
o
o
f
-
=
Lf
Ao
Af
Lo
Adapted from Fig. 6.13, Callister & Rethwisch 8e.
Engineering tensile strain, e
E
ngineering
tensile
stress, s
smaller %EL
larger %EL
In general, for a given material, above two measures of ductility will be different.
https://www.youtube.com/watch?v=MyksI4O26G4

## Slide 27
Temperature Dependence
Modulus of elasticity: Temp. Independent
Yield strength & Tensile strength: Decline with temp. increase
Ductility: Increases with temp. increase

## Slide 28: Toughness
• Energy to break a unit volume of material
• Approximate by the area under the stress-strain curve.
Brittle fracture: elastic energy Ductile fracture: elastic + plastic energy
Adapted from Fig. 6.13, Callister & Rethwisch 8e.
very small toughness
(unreinforced polymers)
Engineering tensile strain, e
E
ngineering
tensile
stress, s
small toughness (ceramics)
large toughness (metals)

## Slide 29: Resilience, Ur
Ability of a material to absorb energy during deformation, and recover it upon unloading.
  Energy stored best in elastic region
If we assume a linear stress-strain curve this simplifies to
Adapted from Fig. 6.15, Callister & Rethwisch 8e.
y
y
r
2
1
U
e
s
@
Energy per unit volume.

## Slide 30: Elastic Strain Recovery
Adapted from Fig. 6.17, Callister & Rethwisch 8e.
Stress
Strain
3. Reapply
load
2. Unload
D
Elastic strain
recovery
1. Load
syo
syi
https://www.youtube.com/watch?v=tmwt6Yaj9yk

## Slide 31: Summary
• Stress and strain: These are size-independent
measures of load and displacement, respectively.
• Elastic behavior: This reversible behavior often
shows a linear relation between stress and strain.
To minimize deformation, select a material with a
large elastic modulus (E or G).
• Toughness: The energy needed to break a unit
volume of material.
• Ductility: The plastic strain at failure.
• Plastic behavior: This permanent deformation
behavior occurs when the tensile (or compressive)
uniaxial stress reaches sy.

## Slide 32: tableun_06_p186
tableun_06_p186
E = 2G (1+ ν)